## Slide 1: Hybrid III-V/Si Modulator
Qiangsheng Huang
August/30/2015

## Slide 2: Schematic description of absorption in quantum wells
Ee1
Ehh1
EF
E=0
E<0
Ee1
Ehh1
EF
|ϕe1|2
|ϕhh1|2
|ϕhh1|2
|ϕe1|2
E>0
|ϕe1|2
|ϕhh1|2
Quantum Confined Stark Effects (QCSE)
The exciton absorption peak red shifts, in the reverse bias.
Band Filling Effects (BFE)
Ee1
Ehh1
EF
The exciton absorption peak blue shifts, in the forward bias.
Gabriela Livescu, et. al., “Free carrier and many-body effects in absorption spectra of modulation-doped quantum wells”, IEEE Journal of Quantum Electronics, vol. 24, No. 8, 1988

## Slide 3: Absorption Spectra
QCSE
BFE
The absorption peak blue shifts linearly as a function of voltage
The absorption peak red shifts quadratically as a function of voltage
Experimental Results
50nm/V

## Slide 4: Absorption Spectra
QCSE
BFE
The absorption peak blue shifts linearly as a function of voltage
The absorption peak red shifts quadratically as a function of voltage
Experimental Results
Simulation Results
QCSE
BFE

## Slide 5: DC Property and RF Property
Chart: Bias (V)
@1550nm
Bias: 0.6V; Vpp: 50mV;
Exciton transitions absorption
Continuum transtions absorption

## Slide 6: The Speed is limited by the carrier lifetime
Carrier lifetime
How to Improve the Speed ?
We can use n-doped MQW to move the work position to the reverse bias.
In this way, can we reduce the carrier lifetime?
Carrier lifetime τ ≈ 1ns
Bandwidth~1GHz